The 230 Space Groups

Prepared by

Kenneth J. De Nault

Department of Earth Science

University of Northern Iowa

## Revised 10/01/2007

## Table of Contents

Crystallographic Systems	2

Triclinic System	2

Monoclinic System	2

2nd Setting: b = 2 or(2	2

1st Setting: c = 2 or(2	2

Orthorhombic System	3

Tetragonal System	4

Trigonal System	6

Hexagonal System	7

Isometric System	8

Descriptions of the 230 Space Groups	9

# Crystallographic Systems

## Triclinic System

The triclinic system consists of three non-orthogonal axes, a, b, and c.  Furthermore, if a( = b( = c(, then (, (, and ( cannot be equal.

- P1

- P(1

## Monoclinic System

The monoclinic system consists of three axes, a, b, and c.  The angles ( and ( are 90( but ( does not equal 90(.  In addition, if a( = b( then ( cannot equal 120(.

In the short form of the second setting, the first character after the space lattice designation refers to the b crystallographic axis, [010].  In the short form or the first setting, the first letter after the space lattice designation refers to the c crystallographic axis, [001].  In the long form of both the second and first settings, the first character after the space lattice designation refers to the a crystallographic axis, [100], the second character refers to the b crystallographic axis, [010], and the third character refers to the c crystallographic axis, [001].  In the long form, the “1” is simply a placeholder to show the position of the 2-fold axis.

### 2nd Setting: b = 2 or(2

Short form	Long form

- P2	P121

- P21	P1211

- C2	C121

- Pm	P1m1

- Pc	P1c1

- Cm	C1m1

- Cc	C1c1

- P2/m	P12/m1

- P21/m	P121/m1

- C2/m	C12/m1

- P2/c	P12/c1

- P21/c	P121/c1

- C2/c	C12/c1

### 1st Setting: c = 2 or(2

Short form	Long form

- P2	P112

- P21	P1121

- B2	B112

- Pm	P11m

- Pb	P11b

- Bm	B11m

- Bb	B11b

- P2/m	P112/m

- P21/m	P1121/m

- B2/m	B112/m

- P2/b	P112/b

- P21/b	P1121/b

- B2/b	B112/b

## Orthorhombic System

The orthorhombic system consists of three orthogonal axes, a, b, and c and a( ( b(, b( ( c(, and a( ( c(.  In the orthorhombic system the first character after the space lattice designation refers to the a crystallographic axis, [100], the second character refers to the b crystallographic axis, [010], and the third character refers to the c crystallographic axis, [001].

- P222

- P2221

- P21212

- P212121

- C2221

- C222

- F222

- I222

- I212121

- Pmm2

- Pmc21

- Pcc2

- Pma2

- Pca21

- Pnc2

- Pmn21

- Pba2

- Pna21

- Pnn2

- Cmm2

- Cmc21

- Ccc2

- Amm2

- Abm2

- Ama2

- Aba2

- Fmm2

- Fdd2

- Imm2

- Iba2

- Ima2	Abbreviated notation

- P2/m2/m2/m	Pmmm

- P2/n2/n2/n	Pnnn

- P2/c2/c2/m	Pccm

- P2/b2/a2/n	Pban

- P21/m2/m2/a	Pmma

- P2/n21/n2/a	Pnna

- P2/m2/n21/a	Pmna

- P21/c2/c2/a	Pcca

- P21/b21/a2/m 	Pbam

- P21/c21/c2/n	Pccn

- P2/b21/c21/m	Pbcm

- P21/n21/n2/m	Pnnm

- P21/m21/m2/n	Pmmn

- P21/b2/c21/n	Pbcn

- P21/b21/c21/a	Pbca

- P21/n21/m21/a	Pnma

- C2/m2/c21/m	Cmcm

- C2/m2/c21/a	Cmca

- C2/m2/m2/m	Cmmm

- C2/c2/c2/m	Cccm

- C2/m2/m2/a	Cmma

- C2/c2/c2/a	Ccca

- F2/m2/m2/m	Fmmm

- F2/d2/d2/d	Fddd

- I2/m2/m2/m	Immm

- I2/b2/a2/m	Ibam

- I2/b2/c2/a	Ibca

- I2/m2/m2/a	Imma

## Tetragonal System

The tetragonal system consists of three orthogonal axes, a, b, and c and a( = b( ( c(.  Because a( = b(, these axes are often named a1 and a2.

In the tetragonal system, the first character after the space lattice designation refers to the c crystallographic axis, [001], the second character refers to the a and b (a1 and a2) crystallographic axes, [010], and the third character refers to the lines located 90( from c and 45( from a and b,  and .

- P4

- P41

- P42

- P43

- I4

- I41

- P(4

- I(4

- P4/m

- P42/m

- P4/n

- P42/n

- I4/m

- I41/a

- P422

- P4212

- P4122

- P41212

- P4222

- P42212

- P4322

- P43212

- I422

- I4122

- P4mm

- P4bm

- P42cm

- P42nm

- P4cc

- P4nc

- P42mc

- P42bc

- I4mm

- I4cm

- I41md

- I41cd

- P(42m

- P(42c

- P(421m

- P(421c

- P(4m2

- P(4c2

- P(4b2

- P(4n2

- I(4m2

- I(4c2

- I(42m

- I(42d	Abbreviated notation

- P4/m2/m2/m	P4/mmm

- P4/m2/c2/c	P4/mcc

- P4/n2/b2/m	P4/nbm

- P4/n2/n2/c	P4/nnc

- P4/m21/b2/m	P4/mbm

- P4/m21/n2/c	P4/mnc

- P4/n21/m2/m	P4/nmm

- P4/n21/c2/c	P4/ncc

- P42/m2/m2/c	P42/mmc

- P42/m2/c2/m	P42/mcm

- P42/n2/b2/c	P42/nbc

- P42/n2/n2/m	P42/nnm

- P42/m21/b2/c	P42/mbc

- P42/m21/n2/m	P42/mnm

- P42/n21/m2/c	P42/nmc

- P42/n21/c2/m	P42/ncm

- I4/m2/m2/m	I4/mmm

- I4/m2/c2/m	I4/mcm

- I41/a2/m2/d	I41/amd

- I41/a2/c2/d	I41/acd

## Trigonal System

The trigonal system has two unique sets of crystallographic axes, hexagonal and rhombohedral.  In the hexagonal system, the first character after the space lattice designation refers to the c crystallographic axis, [0001], the second character refers to the a1, a2, and a3 crystallographic axes, [1000], [0100], and [0010], and the third character refers to the direction 90( from c and 30( from a1 and –a3, .  This latter designation also refers to the direction 90( from c and 30( from a2 and –a1,  and 90( from c and 30( from a3 and –a2, .

In the rhombohedral system, ( =( = ( ( 90( and a( = b( = c(.  Because a( = b( = c(, the axes are often named a1, a2 and a3.

- P3

- P31

- P32

- R3

- P(3

- R(3

- P312

- P321

- P3112

- P3121

- P3212

- P3221

- R32

- P3m1

- P31m

- P3c1

- P31c

- R3m

- R3c	Abbreviated notation

- P(312/m	P(31m

- P(312/c	P(31c

- P(32/m1	P(3m1

- P(32/c1	P(3c1

- R(32/m	R(3m

- R(32/c	R(3c

## Hexagonal System

In the trigonal system, the first character after the space lattice designation refers to the c crystallographic axis, [0001], the second character refers to the a1, a2, and a3 crystallographic axes, [1000], [0100], and [0010], and the third character refers to the direction 90( from c and 30( from a1 and –a3, .  This latter designation also refers to the direction 90( from c and 30( from a2 and –a1,  and the direction 90( from c and 30( from a3 and –a2, .

- P6

- P61

- P65

- P62

- P64

- P63

- P(6

- P6/m

- P63/m

- P622

- P6122

- P6522

- P6222

- P6422

- P6322

- P6mm

- P6cc

- P63cm

- P63mc

- P(6m2

- P(6c2

- P(62m

- P(62c	Abbreviated notation

- P6/m2/m2/m	P6/mmm

- P6/m2/c2/c	P6/mcc

- P63/m2/c2/m	P63/mcm

- P63/m2/m2/c	P63/mmc

## Isometric System

The isometric system consists of three orthogonal axes, a, b, and c and a( = b( = c(.  Because a( = b( = c(, the axes are often named a1, a2 and a3.

In the isometric system, the first character after the space lattice designation refers to the a, b, and c crystallographic axes (a1, a2, and a3), [100], [010], and [001].  The second character refers to the direction [111] and the symmetrically related directions , , and .  The third character refers to the direction [110] and its symmetrically related directions , [011], [101], , and .

- P23

- F23

- I23

- P213

- I213	Abbreviated notation

- P2/m(3	Pm3

- P2/n(3	Pn3

- F2/m(3	Fm3

- F2/d(3	Fd3

- I2/m(3	Im3

- P21/a(3	Pa3

- I21/a(3	Ia3

- P432

- P4232

- F432

- F4132

- I432

- P4332

- P4132

- I4132

- P(43m

- F(43m

- I(43m

- P(43n

- F(43c

- I(43d	Abbreviated notation

- P4/m(32/m	Pm3m

- P4/n(32/n	Pn3n

- P42/m(32/n	Pm3n

- P42/n(32/m	Pn3m

- F4/m(32/m	Fm3m

- F4/m(32/c	Fm3c

- F41/d(32/m	Fd3m

- F41/d(32/c	Fd3c

- I4/m(32/m	Im3m

- I41/a(32/d	Ia3d

# Descriptions of the 230 Space Groups

1	Primitive triclinic space lattice.  The object being repeated has point group symmetry 1.

2	Primitive triclinic space lattice.  The object being repeated has point group symmetry .

3	Primitive monoclinic space lattice.  The object being repeated has point group symmetry 2.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.

4	Primitive monoclinic space lattice.  The object being repeated has point group symmetry 2.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.

5	C face-centered monoclinic space lattice.  The object being repeated has point group symmetry 2.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  There is an identipoint centered in the (001) face (lattice sites ½ ½ 0 and ½ ½ 1).

6	Primitive monoclinic space lattice.  The object being repeated has point group symmetry m.  Perpendicular to the b crystallographic axis is a mirror plane.

7	Primitive monoclinic space lattice.  The object being repeated has point group symmetry m.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ cº parallel to the c crystallographic axis.

8	C face-centered monoclinic space lattice.  The object being repeated has point group symmetry m.  Perpendicular to the b crystallographic axis is a mirror plane.  There is an identipoint centered in the (001) face (lattice sites ½ ½ 0 and ½ ½ 1).

9	C face-centered monoclinic space lattice.  The object being repeated has point group symmetry m.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ cº parallel to the c crystallographic axis.  There is an identipoint centered in the (001) face (lattice sites ½ ½ 0 and ½ ½ 1).

10	Primitive monoclinic space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.

11	Primitive monoclinic space lattice.  The object being repeated has point group symmetry 2/m. Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a mirror plane.

12	C face-centered monoclinic space lattice.  The object being repeated has point group symmetry 2/m. Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  There is an identipoint centered in the (001) face (lattice sites ½ ½ 0 and ½ ½ 1).

13	Primitive monoclinic space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ cº parallel to the c crystallographic axis.

14	Primitive monoclinic space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ cº parallel to the c crystallographic axis.

15	C face-centered monoclinic space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ cº parallel to the c crystallographic axis.  There is an identipoint centered in the (001) face (lattice sites ½ ½ 0 and ½ ½ 1).

16	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

17	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is 2-fold symmetry axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ cº parallel to the c crystallographic axis.

18	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.  Parallel to the c crystallographic axis is 2-fold symmetry axis.

19	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.  Parallel to the c crystallographic axis is 2-fold screw axis with a rotation of 180º and a unit of translation of ½ cº parallel to the c crystallographic axis.

20	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is 2-fold symmetry axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ cº parallel to the c crystallographic axis.  There is an identipoint centered in the (001) face (lattice sites ½ ½ 0 and ½ ½ 1).

21	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

22	Face centered orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

23	Body centered orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

24	Body centered orthorhombic space lattice.  The object being repeated has point group symmetry 222.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.  Parallel to the c crystallographic axis is 2-fold screw axis with a rotation of 180º and a unit of translation of ½ cº parallel to the c crystallographic axis.

25	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

26	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c.  Parallel to the c crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ cº parallel to the c crystallographic axis.

27	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

- Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

- Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

30	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ b( + ½ c(.  Perpendicular to the b crystallographic axis is an axial glide plane with a unit of translation of ½ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

31	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ b(.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counter-clockwise (or clockwise in this case) rotation of 180( and a unit of translation of ½ c(.

32	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is an axial glide plane with a unit of translation of ½ b(.  Perpendicular to the b crystallographic axis is an axial glide plane with a unit of translation of ½ a(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

33	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ b( + ½ c(.  Perpendicular to the b crystallographic axis is an axial glide plane with a unit of translation of ½ a(.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counter-clockwise (or clockwise in this case) rotation of 180( and a unit of translation of ½ c(.

34	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ b( + ½ c(.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

35	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

36	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counter-clockwise (or clockwise in this case) rotation of 180( and a unit of translation of ½ c(.

37	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ c( parallel to the c crystallographic axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

38	A-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

39	A-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

40	A-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

41	A-face centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic is a b axial glide plane with a unit of translation ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

42	Face-centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

43	Face-centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a diamond glide plane with a unit of translation ¼ b( + ¼ c(.  Perpendicular to the b crystallographic axis is a diamond glide plane with a unit of translation of ¼ a( + ¼ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

44	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

45	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

46	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry mm2.  Perpendicular to the a crystallographic axis is a mirror plane.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.

47	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

48	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation ½ b( + ½ c(.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation ½ a( + ½ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a unit of translation ½ a( + ½ b(.

49	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

50	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ b(.

51	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

52	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ b( + ½ c(.  Parallel to the b crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a axis.

53	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ c(.  Parallel to the c crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

54	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

55	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

56	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ b(.

57	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is b axial glide plane with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a 180( counterclockwise (or clockwise) rotation and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.

58	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation ½ b( + ½ c(.  Parallel to the b crystallographic axis is a 2-fold screw axis with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation ½ a( + ½ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

59	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180( counterclockwise (or clockwise) and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180( degrees counterclockwise (or clockwise) and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ b(.

60	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a unit of translation of ½ a( + ½ b(.

61	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

62	Primitive orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ b( + ½ c(.  Parallel to the b crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

63	C-Face centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.

64	C-Face centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m. Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold screw axis with a counterclockwise (or clockwise) rotation of 180( and a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

65	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

66	C-Face centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

67	C-face centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

68	C-Face centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation of ½ c( in a direction parallel to the c crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

69	Face-centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

70	Face-centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a diamond glide plane with a unit of translation ¼ b( + ¼ c(.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a diamond glide plane with a unit of translation of ¼ a( + ¼ c(.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diamond glide plane with a unit of translation of ¼ a( + ¼ b(.

71	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

72	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is b axial glide plane with a unit of translation of ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

73	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation ½ b( in a direction parallel to the b crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a c axial glide plane with a unit of translation ½ c( in a direction parallel to c.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation ½ a( in a direction parallel to the a crystallographic axis.

74	Body-centered orthorhombic space lattice.  The object being repeated has point group symmetry 2/m2/m2/m.  Parallel to the a crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the a crystallographic axis is a mirror plane.  Parallel to the b crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the b crystallographic axis is a mirror plane.  Parallel to the c crystallographic axis is a 2-fold symmetry axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ a( in a direction parallel to the a crystallographic axis.

75	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.

76	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4.  Parallel to the c crystallographic axis is a 4-fold screw axis with a counterclockwise rotation of 90º and a unit of translation of ¼ cº parallel to the c crystallographic axis.

77	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4.  Parallel to the c crystallographic axis is a 4-fold screw axis with a counterclockwise rotation of 90º and a unit of translation of ½ cº parallel to the c crystallographic axis.

78	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4.  Parallel to the c crystallographic axis is a 4-fold screw axis with a counterclockwise rotation of 90º and a unit of translation of ¾ cº parallel to the c crystallographic axis.

79	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.

80	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4.  Parallel to the c crystallographic axis is a 4-fold screw axis with a counterclockwise rotation of 90º and a unit of translation of ¼ cº parallel to the c crystallographic axis.

81	Primitive tetragonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.

82	Body centered tetragonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.

83	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

84	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.

85	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.

86	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.

87	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.

88	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a unit of translation of ¼ cº parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an axial glide plane with a unit of translation of ½ aº parallel to the a crystallographic axis.

89	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Parallel to the a and b crystallographic axes are 2-fold axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

90	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Parallel to the a crystallographic axis is a 2-fold screw axes with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

91	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¼ cº in a direction parallel to the c crystallographic axis.  Parallel to the a and b crystallographic axes are 2-fold axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

92	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¼ cº in a direction parallel to the c crystallographic axis.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

93	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the a and b crystallographic axes are 2-fold axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

94	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

95	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¾ cº in a direction parallel to the c crystallographic axis.  Parallel to the a and b crystallographic axes are 2-fold axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

96	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¾ cº in a direction parallel to the c crystallographic axis.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº parallel to the b crystallographic axis.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

97	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Parallel to the a and b crystallographic axes are 2-fold axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

98	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 422.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¼ cº in a direction parallel to the c crystallographic axis.  Parallel to the a and b crystallographic axes are 2-fold axes.  Parallel to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

99	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the a and b crystallographic axes are mirror planes.  Perpendicular to the direction halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

100	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

101	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the direction halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

102	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ cº + ½ bº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation of ½ cº + ½ aº.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

103	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

104	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a unit of translation of ½ cº + ½ bº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a unit of translation of ½ cº + ½ aº.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

105	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the a and b crystallographic axes are mirror planes.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

106	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the a crystallographic axes is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axes is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

107	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the a and b crystallographic axes are mirror planes.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

108	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

109	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¼ cº parallel to the c crystallographic axis.  Perpendicular to the a and b crystallographic axes are mirror planes.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are diamond glide planes with a translation of ¼ aº + ¼ bº + ¼ cº.

110	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4mm.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a unit of translation of ¼ cº parallel to the c crystallographic axis.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the directions halfway or 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are diamond glide planes with a translation of ¼ aº + ¼ bº + ¼ cº.

- Primitive tetragonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

- Primitive tetragonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

113	Primitive tetragonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

114	Primitive tetragonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Parallel to the a crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the b crystallographic axis is a 2-fold screw axis with a rotation of 180º and a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

115	Primitive tetragonal space lattice.  The object being repeated has point group symmetry m2.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

116	Primitive tetragonal space lattice.  The object being repeated has point group symmetry m2.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit to translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

117	Primitive tetragonal space lattice.  The object being repeated has point group symmetry m2.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

118	Primitive tetragonal space lattice.  The object being repeated has point group symmetry m2.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a translation of ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ cº.  Parallel to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

119	Body centered tetragonal space lattice.  The object being repeated has point group symmetry m2.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

120	Body centered tetragonal space lattice.  The object being repeated has point group symmetry m2.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

121	Body centered tetragonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are mirror planes.

122	Body centered tetragonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 4-fold axis of rotary inversion.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the directions 45º from the a and b crystallographic axes and 90º from the c crystallographic axis are diamond glide planes with a translation of ¼ aº + ¼ bº + ¼ cº.

123	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

124	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and c crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the lines that are perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these lines are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

125	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axes.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions that are perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

126	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a diagonal glide plane with translation ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with translation ½ aº + ½ cº.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

127	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

128	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axes is a diagonal glide plane with translation ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with translation ½ aº + ½ cº.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

129	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with translation ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

130	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with translation ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

131	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

132	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

133	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

134	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a translation of ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ cº.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

135	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

136	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a translation of ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ cº.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

137	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

138	Primitive tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a rotation of 90º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

139	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axis are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions that are perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

140	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a and b crystallographic axis are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendicular to these 2-fold axes are mirror planes.

141	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a 90º counterclockwise rotation and a translation of ¼ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the a and b crystallographic axis are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are mirror planes.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendiculars to these 2-fold axes are diamond glide planes with a translation of ¼ aº + ¼ bº + ¼ cº.

142	Body centered tetragonal space lattice.  The object being repeated has point group symmetry 4/m2/m2/m.  Parallel to the c crystallographic axis is a 4-fold screw axis with a 90º counterclockwise rotation and a translation of ¼ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is an a axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the a and b crystallographic axis are 2-fold symmetry axes.  Perpendicular to the a and b crystallographic axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions perpendicular to the c crystallographic axis and 45º from the a and b crystallographic axes are 2-fold symmetry axes.  Perpendiculars to these 2-fold axes are diamond glide planes with a translation of ¼ aº + ¼ bº + ¼ cº.

143	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.

144	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3.  Parallel to the c crystallographic axis is a 3-fold screw axis with a rotation of 120º counterclockwise and a unit of translation of 1/3 cº parallel to the c crystallographic axis.

145	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3.  Parallel to the c crystallographic axis is a 3-fold screw axis with a rotation of 120º counterclockwise and a unit of translation of 2/3 cº parallel to the c crystallographic axis.

146	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry 3.  Parallel to the direction trisecting the a, b, and c crystallographic axes is a 3-fold symmetry axis.  The objects 3-fold symmetry axis is parallel to this 3-fold axis symmetry axis.

147	Primitive hexagonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 3-fold axis of rotary inversion.

148	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry .  Parallel to the direction trisecting the a, b, and c crystallographic axes is a 3-fold axis of rotary inversion.  The objects 3-fold axis of rotary inversion is parallel to this 3-fold axis of rotary inversion.

149	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 32.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.  Parallel to the directions 30º from the a1, a2, and a3 crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

150	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 32.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.

151	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 32.  Parallel to the c crystallographic axis is a 3-fold screw axis with a rotation of 120º counterclockwise and a unit of translation of 1/3 cº in the direction of parallel to the c crystallographic axis.  Parallel to the directions 30º from the a1, a2, and a3 crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

152	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 32.  Parallel to the c crystallographic axis is a 3-fold screw axis with a rotation of 120º counterclockwise and a unit of translation of 1/3 cº in the direction of parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.

153	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 32.  Parallel to the c crystallographic axis is a 3-fold screw axis with a rotation of 120º counterclockwise and a unit of translation of 2/3 cº in the direction parallel to the c crystallographic axis.  Parallel to the directions 30º from the a1, a2, and a3 crystallographic axes and 90º from the c crystallographic axis are 2-fold symmetry axes.

154	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 32.  Parallel to the c crystallographic axis is a 3-fold screw axis with a rotation of 120º counterclockwise and a unit of translation of 2/3 cº in the direction parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.

155	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry 32.  Parallel to the direction trisecting the a, b, and c crystallographic axes is a 3-fold symmetry axis.  The objects 3-fold symmetry axis is parallel to this 3-fold symmetry axis.  Perpendicular to the direction trisecting the a, b, and c crystallographic axes and parallel to the directions halfway between the individual a, b, and c crystallographic axes are 2-fold symmetry axes.

156	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.

157	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.  Perpendicular to the directions 30º from the a1, a2, and a3 crystallographic axes and 90º from the c crystallographic axis are mirror planes.

158	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

159	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the c crystallographic axis is a 3-fold symmetry axis.  Perpendicular to the directions 30º from the a1, a2, and a3 crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

160	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the direction trisecting the a, b, and c crystallographic axes is a 3-fold symmetry axis.  The objects 3-fold symmetry axis is parallel to this 3-fold axis symmetry axis.  Perpendicular to the direction 90º from the direction trisecting the a, b, and c crystallographic axes and parallel to the directions halfway between the individual a, b, and c crystallographic axes are mirror planes.

161	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry 3c.  Parallel to the direction trisecting the a, b, and c crystallographic axes is a 3-fold symmetry axis.  The objects 3-fold symmetry axis is parallel to this 3-fold axis symmetry axis.

162	Primitive hexagonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 3-fold axis of rotary inversion.  Perpendicular to the directions 30º from a1, a2, and a3 and 90º from the c crystallographic axis are mirror planes.

163	Primitive hexagonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 3-fold axis of rotary inversion.  Perpendicular to the directions 30º from the a1, a2, and a3 crystallographic axes and 90º from the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

164	Primitive hexagonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 3-fold axes of rotary inversion.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.

165	Primitive hexagonal space lattice.  The object being repeated has point group symmetry m.  Parallel to the c crystallographic axis is a 3-fold axes of rotary inversion.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

166	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry (32/m.

167	Primitive rhombohedral space lattice.  The object being repeated has point group symmetry (32/c.

168	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.

169	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation of 1/6 cº parallel to the c crystallographic axis.

170	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation of 5/6 cº parallel to the c crystallographic axis.

171	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation of 1/3 cº parallel to the c crystallographic axis.

172	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation of 2/3 cº parallel to the c crystallographic axis.

173	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation of ½ cº parallel to the c crystallographic axis.

174	Primitive hexagonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 6-fold axis of rotary inversion.

175	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6/m.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.

176	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6/m.  Parallel to the c crystallographic axis is a 6-fold screw axis with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.

177	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 622.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

178	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 622.  Parallel to the c crystallographic axis is a 6-fold screw axis with a unit of rotation of 60º counterclockwise and a translation of 1/6 cº in a direction parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

179	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 622.  Parallel to the c crystallographic axis is a 6-fold screw axis with a unit of rotation of 60º counterclockwise and a translation of 5/6 cº in a direction parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

180	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 622.  Parallel to the c crystallographic axis is a 6-fold screw axis with a unit of rotation of 60º counterclockwise and a translation of 1/3 cº in a direction parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

181	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 622.  Parallel to the c crystallographic axis is a 6-fold screw axis with a unit of rotation of 60º counterclockwise and a translation of 2/3 cº in a direction parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

182	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 622.  Parallel to the c crystallographic axis is a 6-fold screw axis with a unit of rotation of 60º counterclockwise and a translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

183	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6mm.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.  Perpendicular to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are mirror planes.

184	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6mm.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are c axial glide planes with a unit of translation ½ cº in a direction parallel to the c crystallographic axis.

185	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6mm.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are mirror planes.

186	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6mm.  Parallel to the c crystallographic axis is a 6-fold screw axis with a rotation of 60º counterclockwise and a unit of translation ½ cº in a direction parallel to the c crystallographic axis.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.  Perpendicular to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are c axial glide planes with a unit of translation ½ cº in a direction parallel to the c crystallographic axis.

187	Primitive hexagonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 6-fold symmetry axis of rotary inversion.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

188	Primitive hexagonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 6-fold symmetry axis of rotary inversion.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.

189	Primitive hexagonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 6-fold symmetry axis of rotary inversion.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Perpendicular to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are mirror planes.

190	Primitive hexagonal space lattice.  The object being repeated has point group symmetry .  Parallel to the c crystallographic axis is a 6-fold symmetry axis of rotary inversion.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Perpendicular to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

191	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6/m2/m2/m.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.  Perpendicular to these axes are mirror planes.

192	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6/m2/m2/m.  Parallel to the c crystallographic axis is a 6-fold symmetry axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.  Perpendicular to these directions are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

193	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6/m2/m2/m.  Parallel to the c crystallographic axis is a 6-fold screw axis with a counterclockwise rotation of 60º and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Perpendicular to the a1, a2, and a3 symmetry axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.  Perpendicular to these axes are mirror planes.

194	Primitive hexagonal space lattice.  The object being repeated has point group symmetry 6/m2/m2/m.  Parallel to the c crystallographic axis is a 6-fold screw axis with a counterclockwise rotation of 60º and a unit of translation of ½ cº parallel to the c crystallographic axis.  Perpendicular to the c crystallographic axis is a mirror plane.  Parallel to the a1, a2, and a3 symmetry axes are 2-fold symmetry axes.  Perpendicular to the a1, a2, and a3 symmetry axes are mirror planes.  Parallel to the directions 30º to a1, a2, and a3 and 90º to the c crystallographic axis are 2-fold symmetry axes.  Perpendicular to these axes are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

195	Primitive isometric space lattice.  The object being repeated has point group symmetry 23.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Along the lines corresponding to the body diagonal of a cube are 3-fold symmetry axes.

196	Face centered isometric space lattice.  The object being repeated has point group symmetry 23.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Along the lines corresponding to the body diagonal of a cube are 3-fold symmetry axes.

197	Body centered isometric space lattice.  The object being repeated has point group symmetry 23.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Along the lines corresponding to the body diagonal of a cube are 3-fold symmetry axes.

198	Primitive isometric space lattice.  The object being repeated has point group symmetry 23.  Parallel to the a, b, and c crystallographic axes are 2-fold screw axis a rotation of 180( and a translation of aº/2 parallel to the a crystallographic axis.  Along the lines corresponding to the body diagonal of a cube are 3-fold symmetry axes.

199	Body centered isometric space lattice.  The object being repeated has point group symmetry 23.  Parallel to the a, b, and c crystallographic axes are 2-fold screw axes with a rotation of 180( and translation of aº/2 parallel to the a crystallographic axis.  Parallel to the lines corresponding to the four body diagonals of a cube are 3-fold symmetry axes.

200	Primitive isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Perpendicular to these axes are mirror planes.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

201	Primitive isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a axis is a diagonal glide plane with translation of ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with translation of ½ aº + ½ cº.  Perpendicular to the c crystallographic axis is a diagonal glide plane with translation ½ aº + ½ bº.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

202	Face centered isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Perpendicular to these axes are mirror planes.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

203	Face centered isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Perpendicular to the a axis is a diamond glide plane with translation of ¼ bº + ¼ cº.  Perpendicular to the b crystallographic axis is a diamond glide plane with translation of ¼ aº + ¼ cº.  Perpendicular to the c crystallographic axis is a diamond glide plane with translation of ¼ aº + ¼ bº.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

204	Body centered isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold symmetry axes.  Perpendicular to these axes are mirror planes.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

205	Primitive isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold screw axes with a 180( rotation and a translation of ½ a(.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a (or c, see footnote) axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Perpendicular to the c crystallographic axis is an a (or b, see footnote) axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

206	Body centered isometric space lattice.  The object being repeated has point group symmetry 2/m.  Parallel to the a, b, and c crystallographic axes are 2-fold screw axes with a 180( rotation and a translation of ½ a(.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a (or c, see footnote) axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Perpendicular to the c crystallographic axis is an a (or b, see footnote) axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold axes of rotary inversion.

207	Primitive isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

208	Primitive isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axis with 90º counterclockwise rotation and a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

209	Face centered isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

210	Face centered isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axis with 90º counterclockwise rotation and a unit of translation of ¼ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

211	Body centered isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

212	Primitive isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axis with 90º counterclockwise rotation and a unit of translation of ¾ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

213	Primitive isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axis with 90º counterclockwise rotation and a unit of translation of ¼ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

214	Body centered isometric space lattice.  The object being repeated has point group symmetry 432.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axis with 90º counterclockwise rotation and a unit of translation of ¼ aº in a direction parallel to the a crystallographic axis.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Parallel to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are 2-fold symmetry axes.

215	Primitive isometric space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes of rotary inversion.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Perpendicular to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are mirror planes.

216	Face centered isometric space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes of rotary inversion.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Perpendicular to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are mirror planes.

217	Body centered isometric space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes of rotary inversion.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Perpendicular to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are mirror planes.

218	Primitive isometric space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes of rotary inversion.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Perpendicular to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are diagonal glide planes with a translation of ½ aº + ½ bº + ½ cº.

219	Face centered isometric space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes of rotary inversion.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Perpendicular to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

220	Body centered isometric space lattice.  The object being repeated has point group symmetry 3m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes of rotary inversion.  Parallel to the directions corresponding to the four body diagonals of a cube are 3-fold symmetry axes.  Perpendicular to the directions corresponding to the six lines joining the midpoints of opposite edges of a cube are diamond glide planes with a translation of ¼ aº + ¼ bº + ¼ cº.

221	Primitive isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to these 4-fold axes are mirror planes.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are mirror planes.

222	Primitive isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a translation of ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ cº.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are diagonal glide planes with translation ½ aº + ½ bº + ½ cº.

223	Primitive isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to these 4-fold axes are mirror planes.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are diagonal glide planes with translation ½ aº + ½ bº + ½ cº.

224	Primitive isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to the a crystallographic axis is a diagonal glide plane with a translation of ½ bº + ½ cº.  Perpendicular to the b crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ cº.  Perpendicular to the c crystallographic axis is a diagonal glide plane with a translation of ½ aº + ½ bº.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are mirror planes.

225	Face centered isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to these 4-fold axes are mirror planes.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are mirror planes.

226	Face centered isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to these 4-fold axes are mirror planes.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

227	Face centered isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axes with a counterclockwise rotation of 90( and a translation of ½ a(.  Perpendicular a crystallographic axis is a diamond glide plane with a translation of ¼ bº + ¼ cº.  Perpendicular to the b crystallographic axis is a diamond glide plane with a translation of ¼ aº + ¼ cº.  Perpendicular to the c crystallographic axis is a diamond glide plane with a translation of ¼ aº + ¼ bº.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are mirror planes.

228	Face centered isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axes with a counterclockwise rotation of 90( and a translation of ½ a(.  Perpendicular a crystallographic axis is a diamond glide plane with a translation of ¼ bº + ¼ cº.  Perpendicular to the b crystallographic axis is a diamond glide plane with a translation of ¼ aº + ¼ cº.  Parallel to the c crystallographic axis is a diamond glide plane with a translation of ¼ aº + ¼ bº.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are c axial glide planes with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

229	Body centered isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold symmetry axes.  Perpendicular to these 4-fold axes are mirror planes.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are mirror planes.

230	Body centered isometric space lattice.  The object being repeated has point group symmetry 4/m2/m.  Parallel to the a, b, and c crystallographic axes are 4-fold screw axes with a counterclockwise rotation of 90( and a translation of ½ a(.  Perpendicular to the a crystallographic axis is a b axial glide plane with a unit of translation of ½ bº in a direction parallel to the b crystallographic axis.  Perpendicular to the b crystallographic axis is an a (or c, see footnote) axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Perpendicular to the c crystallographic axis is an a (or b, see footnote) axial glide plane with a unit of translation of ½ aº in a direction parallel to the a crystallographic axis.  Parallel to the direction so the four body diagonals of a cube are 3-fold axes of rotary inversion.  Parallel to the directions corresponding to the six lines joining the midpoints of the opposite edges of a cube are 2-fold symmetry axes.  Perpendicular to these lines are diamond glide planes with translations of ¼ aº + ¼ bº + ¼ cº.

# Footnotes

The term orthogonal means at right angles (90().  The term non-orthogonal means not at right angles (( 90().

Orthogonal means the axes are at right angles, ( = 90(, ( = 90(, and ( = 90(.

This space group has three variations; the one described, one with the 2-fold screw axis parallel to the a crystallographic axis, P2122, and one with the 2-fold screw axis parallel to the b crystallographic axis, P2212.

This space group has three variations; the one described, one with the 2-fold symmetry axis parallel to the a crystallographic axis, P22121 and one with the 2-fold symmetry axis parallel to the b crystallographic axis, P21221.

This space group has three variations; the one described, an A-face centered orthorhombic space lattice with a 2-fold screw axis parallel to the a crystallographic axis and 2-fold symmetry axes parallel to the b and c crystallographic axes, C2122, and a B-face centered orthorhombic space lattice with a 2-fold axis parallel to the a and c crystallographic axes and a 2-fold screw axis parallel to the b crystallographic axis, C2212.

This space group has three variations; the one described, an A-face centered space lattice, A222, and a B-face centered space lattice, B222.

This space group has three variations; the one described, one with the 2-fold symmetry axis parallel to the a crystallographic axis, P2mm, and one with the 2-fold symmetry axis parallel to the b crystallographic axis, Pm2m.

This space group has six variations; the one described, Pcm21, Pc21m, Pm21c, P21mc, and P21cm.

This space group has three variations; the one described Pc2c and P2cc.

Because the c crystallographic axis is a 4-fold symmetry axis, the a and b crystallographic axes are identical.  Thus, this could also be described as a c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

Because the c crystallographic axis is a 4-fold symmetry axis, the a and b crystallographic axes are identical.  Thus, this could also be described as a c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.

Because the a crystallographic axis is a 4-fold symmetry axis, the b and c crystallographic axes are identical.  Thus, this could also be described as a c axial glide plane with a unit of translation of ½ cº in a direction parallel to the c crystallographic axis.